EPOXY ADHESIVES

## FOR ELECTRONIC AND INDUSTRIAL APPLICATIONS

INSULATIVE ADHESIVES

EPOXY -13      MOISTURE RESISTANT

EPOXY -14      HIGH THERMAL CONDUCTIVITY

EPOXY -15      HIGH PEEL

EPOXY -16      HIGH PEEL

EPOXY -17      HIGH PEEL, HIGH THERMAL CONDUCTIVITY

EPOXY -20	      OPTICAL EPOXY, RADIATION RESISTANT

EPOXY -30      OPTICAL EPOXY, RADIATION RESISTANT

EPOXY -50      OPTICALLY CLEAR ADHESIVE SEALANT

GENERAL PURPOSE EPOXIES

CONDUCTIVE ADHESIVES

OHMEX AG                            THERMOSETTING SILVER FOR OHMIC

BONDING

SILVER EPOXY PASTE       SCREENABLE THERMOSETTING SILVER

SILVER BOND                       LOW TEMPERATURE THERMOSETTING

SILVER SYSTEMS

MICROCIRCUIT SILVER    100% SOLIDS AND LOW TEMPERATURE

CURING SYSTEMS

GOLD EPOXY PASTE          ONE-PART AND TWO -PART GOLD FILLED

SYSTEMS

POLYIMIDE DIE ATTACH  LOW MOBILE ION, SILVER FILLED ADHESIVE

FOR IC CHIP BONDING

SURFACE MOUNT                LOW COST, HIGH DENSITY FOR INTEGRATED

ADHESIVE                              CIRCUITS

NANOPOXY 60                       LONG POT LIFE, FAST CURE FOR NANOSCALE

ELECTRONICS

TRANSENE CO. INC. 10 ELECTRONICS AVE. DANVERS MA 01923 978-777-7860-FAX 739-5640 www.transene.com

INSUL-BOND EPOXY ADHESIVES

ONE-PART LOW TEMPERATURE CURING SYSTEMS

Insul-bond Adhesives are solvent-free, low gassing epoxy formulations recommended for discreet component attachment, substrate mounting and lid sealing in the production of high reliability hybrid microcircuits. These adhesives provide multiple bonding of chips or components in a single operation while maintaining low processing temperatures. Subsequent thermal compression or ultrasonic bonding operations are feasible.

Insul-Bond Epoxy 13, 14 and 15 maintain minimal outgassing, high electrical resistivity and high bond strength to 200oC operating temperatures. Compatibility with aluminum and other metallizations common to microelectronic devices is assured.

Properties of Insul-Bond Adhesives

|  | Epoxy 13 | Epoxy 14 | Epoxy 15 |
| --- | --- | --- | --- |
| Physical (Uncured) |  |  |  |
| Composition | 1-part/filled | 1-part/filled | 1-part/filled |
| Color | Buff | Buff | Buff |
| Solids | 100% | 100% | 100% |
| Viscosity cps | Thixotropic paste | Thixotropic paste | Thixotropic paste |
| Shelf life | 6 months | 6 months | 6 months |
| Physical (Cured) Thermal Conductivity BTU/hr/ft2/in/oF | 4 | 12 | 4 |
| Coef. Thermal Expansion in/in/oC/x 10-6 | 30 | 23 | 30 |
| Outgassing (post cure) 1000 hrs @ 125oC | 0.4% | 0.35% | 0.4% |
| Moisture Absorption 7 days immersion 25oC | 0.05% | 0.16% | 0.05% |
| Bond Strength (lap shear @ 25oC) 125oC to 1000 HRS 30 Days H20 immersion | 2000 1500 2000 | 1500 1000 1500 | 2000 1500 ------ |
| Service Temp. Range continuous | -40oC + 150oC | -40oC to 150oC | -40oC to +150oC |
| Electrical (cured) |  |  |  |
| Volume Resistivity(ohm-cm) | 1x1015 | 1x1016 | 1 x1015 |
| Dissipation Factor (1 mc) | 0.01 | 0.02 | 0.01 |
| Dielectric Constant(1 mc) | 3.9 | 4.4 | 3.9 |
| Dielectric Strength(v/mil) | 450 | 450 | 450 |

APPLICATION:

Selection of Insul-Bond Epoxy 13, 14 or 15 is made on the basis of thermal conductivity and thermal expansion requirements. Application by screen printing technique (180-225 mesh screen) or automatic dispensing is suggested. For maximum bond strengths and reproducibility, adhesive thickness of 1.5-2.0 mil is recommended.

CURE SCHEDULE:

FAST-15 min. @ 140oC;   MEDIUM-30 min @ 115oC;   SLOW-1 hr. @ 100oC

TRANSENE COMPANY, INC. 10 Electronics Ave, Danvers Ma. 978-777-7860 fax 739-5640 www.transene.com

INSUL-BOND EPOXY ADHESIVES

Two-Part, Low Temperature Cure,

High Peel Strength Systems

Insul-Bond 16 & 17 adhesives are solvent free, electrically non-conductive epoxy systems designed for die attachment, substrate mounting and lid sealing in hybrid microelectronics applications. These 2-part systems feature rapid cure at very low temperatures and outstanding bond “peel” strengths-typically 10 times greater than those of standard epoxy materials. Application by screen printing (180-225 SS mesh) or automatic dispensing is recommended.

Properties of Insul-Bond Adhesives

|  | Epoxy 16 | Epoxy 17 |
| --- | --- | --- |
| Physical (Uncured) |  |  |
| Composition | Two-part | Two-part |
| Color | Tan | Tan |
| Solids | 100% | 100% |
| Viscosity. cps | 80,000 cps | 80,000 cps |
| Shelf life | 6 months | 4 months |
| Pot life | >2hours | >2 hours |
| Mixing Ratio by weight A:B | 100(A)/7(B) | 100(A)/7(B) |
| Physical (Cured) |  |  |
| Bond Strength |  |  |
| Sheer | 2,000 psi | 2,000 psi |
| Peel | 80 pli | 80 pli |
| Heat Distortion Temp. | > 125oC | > 125oC |
| Outgassing (weight loss) 1000 hrs @ 125oC | 0.35% | 0.35% |
| High Temperature Storage: Peel Strength (125oC) Peel Strength (150oC) | >70 pli >70 pli | >70 pli >70 pli |
| Thermal Conductivity BTU/hr/ft2/in/oF | 4 | 10 |
| Coef. Thermal Expansion in/in/oC/x 10-6 | 35 | 23 |
| Service Temp. Range continuous | -40oC to 150oC | -40oC to +150oC |
| Electrical (cured) |  |  |
| Volume Resistivity(ohm-cm) | 1015 ohm/cm | 1015 ohm/cm |
| Dissipation Factor (1 mc) | .01 | .01 |
| Dielectric Constant(1 mc) | 3.3 | 3.3 |
| Dielectric Strength(v/mil) | 500v/mil | 500 v/mil |

CURE:

Mix in ratio of 100 parts A to 7 parts B(hardner). Select any cure schedule as follows

| 50oC | 20 min. (minimum) | 20 min. (minimum) |
| --- | --- | --- |
| 75oC | 15 min. “ | 15 min. “ |
| 100oC | 10 min. “ | 10 min. “ |

TRANSENE COMPANY, INC. 10 Electronics Ave, Danvers Ma. 978-777-7860 fax 739-5640 www.transene.com

OPTICAL EPOXIES

Radiation Resistant Adhesives for Solar Cells

Epoxy bonding adhesives used in electro-optical applications, and engineered for bonding cover glasses to solar cells in space vehicles.  Also recommended for electro-optical applications.

EPOXY - 20

Two component system

Excellent bonding properties

EPOXY - 30

Three component system

High temperature capability

Greater bonding strength

Features

- High impact resistance

- Flexible elongation properties

- Excellent bonding strength

- Optical clarity

- Resistant to radiation darkening

Transene Co. Inc.  10 Electronics Ave, Danvers, MA 01923 Tel:  978-777-7860 Fax 978-739-5640 www.transene.com

Optical Epoxies

DESCRIPTION

Epoxy -20 Adhesive is a special bonding material designed and formulated for electro-optical applications requiring high light transmission and resistance to radiation darkening. Structurally, Epoxy -20 is a crossed polymer of bisphenol poly-glycol epoxide, supplied as a two component system. The product is characterized by high impact resistance, elongation properties with a degree of flexibility and excellent bonding properties. It cures at room temperature or at elevated temperature.

Epoxy -30 Adhesive is a bisphenol poly-glycol anhydride epoxide system and offers higher temperature capability and greater bonding strength. It is supplied as a 3-component system.

PROPERTIES OF OPTICAL EPOXIES

|  | EPOXY - 20 | EPOXY -30 |
| --- | --- | --- |
| Color(Gardner) | <1 | <1 |
| Gamma Radiation Resist | >108rads | >108rads |
| Distortion Temperature | 150oC | 200oC |
| Lap Shear Strength | 1200 psi | 1500 psi |
| Shore D Durometer | 75 | 80 |
| Volume Resistivity | 1015ohm cm | 1015ohm cm |
| Dielectric Constant | 3.3 (1 mc) | 3.0 (1 mc) |
| Dissipation Factor | .032 (1 mc) | .021 (1 mc) |
| Storage Life | 6 months (min.) | 6 months (min,) |
| Pot Life | 4 hours (min.) | 4 hours (min.) |
| Cure Temperature | 70oC or rm. temp. | 105oC |
| Refractive Index | 1.54 | 1.57 |
| Light Transmission | 3,000 A cut-off | 3,000 A cut-off |

Application:

Epoxy -20: Mix thoroughly 100 parts of A with 8 parts of B by weight. Avoid entrapment of air bubbles during the mixing process.  Deaeration at reduced pressure is permissible. Apply to clean surfaces. (Solar cells may be cleaned satisfactorily in Transene 100.) Cure the bonded assemblies at 70oC for 5 hours or at room temperature for 4 days.

Epoxy -30: Mix 100 parts A, 70 parts B, and 2 parts of C, all by weight. Warm to obtain a clear mixture, then cool to room temperature. Deaeration at reduced pressure to remove air bubbles is permissible. Apply to clean surfaces; cure at 80oC for 1 hour followed by 2 hours at 150oC.

Transene Co. Inc.  10 Electronics Ave. Danvers, MA 01923 Tel: 978-777-7860 Fax: 978-739-5640 www.transene.com

EPOXY 50

ADHESIVE SEALANT

EPOXY 50 is formulated as a two-component, low temperature system, designed for use as an adhesive sealant.  The curing system is composed of 100% resin-solids and contains no solvents.

PROPERTIES

| Color | Water clear |
| --- | --- |
| Adhesion-lap shear strength | > 3,000 psi |
| Hardness (Shore D) | 80 |
| HDT-Distortion Temperature | 100oC |
| Volume Resistivity | 1.2 x 1016 |
| Dielectric Constant | 3.3 @ 1 MC |
| Pot Life | >3 Hours |
| Storage Life | >6 Months |

INSTRUCTIONS:

- Mixing Ratio (by weight): 10 parts A/3.6 parts B

- Cure: Select cure cycle to fit processing

| Temperature oC | Gel Time | Cure Time |
| --- | --- | --- |
| 25 (rm. temp) | 5 hours | 15 hours |
| 50 | 1 hour | 4 hours |
| 75 | 10 minutes | 30 minutes |
| 100 | 5 minutes | 10 minutes |

Transene Company Inc. 10 Electronics Avenue, Danvers MA 01923 Tel: 978-777-7860 Fax: 978-739-5640 www.transene.com

GENERAL PURPOSE EPOXIES

# For Electronic Potting Applications

Newest epoxy materials for potting semiconductor components and electronic assemblies.

EPOXY – 125

Room temperature curing epoxy – for applications to 125oC.

EPOXY – 175

Elevated temperature curing epoxy – for applications to 175oC.

EPOXY – 200

Novalac-epoxy formulation – for applications to 200oC.

Epoxy – 225

Resin-Anhydride epoxy system – for high temperature applications to 225oC.

Transene Co. Inc. 10 Electronics Ave, Danvers MA 01923 Tel: 978-777-7860 Fax: 739-5640 www.transene.com

GENERAL PURPOSE EPOXIES

Description:

General purpose epoxies are formulated as two component systems to provide the best electrical, physical and mechanical properties attainable. The epoxy systems comprise (1) a resin, based upon etho-xyline polymer chemistry, and (2) a reactive hardener to increase linear polymerization and cross-linking of the epoxy resin systems are relatively low in viscosity and contain low-loss filler for improved physical characteristics. Castings, which are shrink free, void free and low in thermal expansion, are easily prepared. The electrical characteristics are not sacrificed.

Applications

General purpose epoxies are recommended for protection and low cost packing of semiconductor components, electronic devices and circuit assemblies. The epoxy compounds meet AIEE classes A-B-C-D-H for electrical potting compounds, as well as MIL specifications.

PROPERTIES OF GENERAL PURPOSE EPOXIES

| Physical Properties | Epoxy –125 | Epoxy –175 | Epoxy –200 | Epoxy –225 |
| --- | --- | --- | --- | --- |
| Color | Black | Black | Black | Black |
| Heat Dist.temp. (oC) | 125 | 175 | 200 | 225 |
| Visc. Mixed (cps) | 2,200 | 38,000 | 20,000 | 4,200 |
| Flex. Str. (psi) | 13,600 | 15,600 | 14,500 | 14,000 |
| Flex.Mod.x 10-5(psi) | 4.08 | 3.37 | 3.90 | 4.4 |
| Comp.Yield Str. (psi) | 15,000 | 15,820 | 35,000 | 18,500 |
| Comp.Mod x 10-5(psi) | 3.40 | 3.10 | 2.60 | 2.89 |
| Tensile Str. (psi) | 11,300 | 10,500 | 10,000 | 10,000 |
| Tens.Mod x 10-5(psi) |  |  | 4.3 | 4.4 |
| Izod Imp. Str.(ft.lbs./in.notch) | 0.3 | 0.33 | 0.50 | 0.48 |
| Hardness, Shore D | 85 | 90 | 90 | 90 |
| Shrinkage (max.) | 1% | 1% | 1% | 1% |
| Thermal Expan.(in/in/oC)x 10-6 | 30 | 30 | 30 | 30 |
| Electrical Properties |  |  |  |  |
| Dielectric Constant |  |  |  |  |
| Frequency, cps 60 | 4.10 | 4.18 | 3.93 | 3.09 |
| Frequency, cps 103 | 3.99 | 4.12 | 3.88 | 3.07 |
| Frequency, cps 106 | 3.39 | 3.57 | 3.47 | 2.91 |
| Dissipation Factor |  |  |  |  |
| Frequency, cps 60 | 0.0099 | 0.005 | 0.0067 | 0.0035 |
| Frequency, cps 103 | 0.023 | 0.015 | 0.015 | 0.0054 |
| Frequency, cps 106 | 0.034 | 0.039 | 0.029 | 0.015 |
| Volume Resist. | 1.19 x 1016 | 1.2 x 1016 | 1.2 x 1016 | 5.8 1016 |
| Surface Resist. | 7.9 x 1015 | 7.8 x 1015 | 7.9 x 1015 | 7.9 x 1015 |
| Dielect. Str. V/mil | 420 | 455 | 585 | 390 |
| Are Resit. (Av.Sec.) |  |  | 120 | 75 |
| Cure Schedule |  |  |  |  |
| Resin:hardner Ratio | 100:17 | 100:12 | 100:10 | 100:45 |
| Pot Life | 1 hr. | 4 hrs. | 4 hrs. | >24Hrs. |
| Initial Gel | 4 hrs @ RT | 2 hrs @ 90oC. | 2 hrs @ 80oC. | 2 hrs @ 90oC. |
| Post-Cure | +48 hrs @ RT | +4 hrs @ 150oC. | +2 hrs @ 150oC. | +4 hrs @ 165oC +16hrs@ 200oC |

Transene Co. Inc. 10 Electronics Ave, Danvers, MA 01923 Tel: 978-777-7860 Fax: 739-5640 www.transene.com

OHMEX - AG

Thermosetting Silver for Ohmic Bonding to Semiconductors

Produces Quality Electrical and Mechanical Contacts

FEATURES

- One - part  system

- High bond strength

- Ohmic contacts

- Low contact resistance

- Low thermal impedance

- Low thermal stress

- Temperature stability -65oC to +275o-C

- Low outgassing

APPLICATIONS

CHIP BONDING - Silicon, germanium and other semiconductor materials - for transistors, diodes, rectifiers, thermistors, integrated monolithic and hybrid circuits.

Also bonds to: glass, metals, ceramic, mica, plastics, graphite, and quartz

FOR PRODUCTION AND LABORATORY USE

# Transene Company Inc. 10 Electronics Avenue, Danvers MA 01923 Tel: 978-777-7860 Fax: 739-5640 www.transene.com

OHMEX - AG

DESCRIPTION

Ohmex-Ag is a conductive silver preparation containing as a bonding constituent silver epoxide. It is supplied in the form of a thin paste, ready to use.  Its composition is unique, providing high conductivity and excellent bonding strength after appropriate cure. OHMEX-Ag is used to advantage in place of lead-tin solder or other alloys to avoid flux contamination or exposure to excessive temperature and for process simplification. OHMEX-Ag produces very low resistance ohmic contacts with all metals and bonds to most insulators. Ohmic bonds are also produced with semiconductors if the surface is first metallized or if the surface is highly “doped” and lapped. OHMEX-Ag finds extensive use in bonding semiconductor ships, integrated monolithic and hybrid circuits, diodes and transistors, and thin films on ceramic substrates - in all types of package configurations.

PROPERTIES

| System | One-Part |
| --- | --- |
| Composition | Silver filled epoxy |
| Density | 2.5 |
| Viscosity | 90,000 cps. |
| Electrical Resistivity, nominal | 5 x 10-4 ohm-cm |
| Thermal Conductivity | 100 BTU/ft2/hr./oF./in. |
| Outgassing | 0.097% @ 100oC (1250 hours) |
|  | 0.7% @ 125oC (1000 hours) |
|  | < 1.2% @ 160oC (1000 hours) |
| Bond Shear Strength | > 1000 PSI |
| Temperature Stability Range | -65oC to + 275oC ( +325oC intermittent) |
| Linear Coef. of Therm Expan. | 5 x 10-5 cm/cm/oC |
| Storage | 40oF or below |
| Shelf Life | 6 months |
| Thinner | Butyl cellosolve acetate |
| Cure Temp. | 150oC (minimum) |

INSTRUCTIONS

Use OHMEX-Ag as supplied. Special thinner is supplied though thinning is unnecessary for most application. Apply OHMEX-Ag to the parts to be bonded, press lightly, then cure in drying oven at 150o - 160oC for at least 15 hours or 1 hour at 150oC followed by at least 1 hour at 265oC.

Special Thinner included

#### Transene Company Inc. 10 Electronics Avenue, Danvers MA 01923 Tel: 978-777-7860 Fax: 739-5640 www.transene.com

SILVER-MET

Silver Metallizations for Non-Metals

Silver-filled, air-drying polymer formulations designed to provide high conductivity metallizations on plastics, paper, mica, ceramic and other non-conductive materials.

SILVER-MET 145

Brush, dip or spray application

SILVER-MET 170

Brush, dip or spray application

High silver density

SILVER-MET 270

Screen print application

SPECIAL APPLICATIONS

- Tantalum capacitor terminations

- Shielding against RF/ EMI

Transene Company, Inc. 10 Electronics Ave. Danvers MA 01923 978-777-7860 fax: 978-739-5640 www.transene.com

SILVER-MET

DESCRIPTION

Transene Silver-Met formulations are silver-filled, air-drying polymers designed to provide high conductivity metallizations on plastics, paper, mica, and other non-conductive surfaces. The silver film allows direct soft-soldering without the use of flux. The film also permits subsequent metallizations through the electroplating process.

Silver-Met is suggested for use in electronics and microwave applications for connectors, contacts, magnetic shielding, capacitor terminations, etc.

The product is most effective for RF /EMI shielding because it reflects as well as absorbs energy. For tantalum capacitors, Silver-Met functions uniquely as terminations for the capacitor.

Properties of Silver-Met

|  | Type 145 | Type 170 | Type 270 |
| --- | --- | --- | --- |
| Application | Dip/ Spray | Dip/ Brush | Screen print |
| Silver Content | 45% | 70% | 70% |
| Viscosity (cps) | 500 | 45,000 | 150,000 |
| Thinner | Butyl Acetate | Butyl Acetate | Butyl Carbitol Acetate |
| Sheet Resistance (milli-ohms/sq/mil) | 160 | 160 | 160 |
| Service Temperature | - 30o to 110o C | - 30o to 110o C | - 30o to 110o C |
| Drying Time @ 25o C | 20 hours | 20 hours | N/A |
| Drying Time @ 80o - 125o C | 1 hour | 1 hour | 1 hour |

APPLICATION

SILVER-MET 145 and SILVER-MET 170 may be applied by brush, dip or spray techniques. After application, substances should be allowed to level and air-dry at room temperature for 1/2 hour to 1 hour, then baked at 80o to 100o C for 1 hour to obtain complete drying.

SILVER-MET 270 may be applied by screen printing using standard 180 to 200 mesh screen. After application substrates should be allowed to level for 5 to 10 minutes, then baked at 80o to 125o C for 1 hour to obtain complete drying.

SILVER-MET 170 and 270 provide a metallic base for direct soft-soldering at temperatures up to 190o C. Types 145, 170, and 270 provide a suitable base for further metallization by electroplating.

Transene Company, Inc. 10 Electronics Ave. Danvers MA 01923 978-777-7860 fax: 978-739-5640 www.transene.com

SILVER EPOXY PASTE

Screenable Thermosetting Silver for Ohmic Bonding

A screenable silver epoxy preparation for developing high  quality electrical and mechanical contacts - used in bonding semiconductors and other devices in hybrid microelectronic circuits.

SILVER EPOXY PASTE - TYPE I

Standard screenable conductive epoxy

SILVER EPOXY PASTE - TYPE II

Screenable conductive compliant epoxy

FEATURES

- One component system

- Excellent screening characteristics

- Develops high bond strength

- Low contact resistance

- Very low thermal stress

- Low thermal impedance

- Temperature -65o to +250oC

Transene Co. Inc.  10 Electronics Ave, Danvers, MA 01923 Tel: 978-777-7860 Fax: 739-5640 www.transene.com

##### SILVER EPOXY PASTE

DESCRIPTION

Silver Epoxy Paste is a one component system designed as a conductive thermosetting silver preparation for screen printing applications. Its composition is unique, providing high electrical and thermal conductivity with excellent bond strength after appropriate cure. Silver Epoxy Paste is used to advantage in place of lead-tin solders to avoid flux contamination or exposure to excessive temperature and for process simplification by screening on contacts.

Silver Epoxy Paste forms ohmic bonds with semiconductors if the surface of the semiconductor is metallized or if the surface is highly “doped” and lapped. The product finds extensive use in bonding semiconductor chips, integrated monolithic circuits, diodes, transistors and other components in thin film and thick film hybrid microelectronic circuits. It bonds to glass, mica, plastic, graphite, quartz and other materials.

PROPERTIES

Silver Epoxy Paste Type I & Type II

| System | One-Part |
| --- | --- |
| Composition | Silver filled epoxy |
| Rheology | Thixotropic paste |
| Viscosity | 90,000 cps. 5% |
| Thinner | Butyl carbitol acetate |
| Cure Temp. | 150oC (minimum) |
| Electrical Resistivity, nominal | 1 x 10-4 ohm-cm |
| Thermal Conductivity | 100 BTU/ft2/hr./oF./in. |
| Bond Shear Strength | 1500 PSI |
| Outgassing | 0.097% @ 100oC (1250 hours) |
|  | 0.7% @ 125oC (1000 hours) |
|  | 1.2% @ 160oC (1000 hours) |
| Temperature Stability Range | -65oC to + 250oC |
| Linear Coef. of Therm Expan. | 5 x 10-5 cm/cm/oC |
| Storage | 40oF or below |
| Shelf Life | 6 months @ 40o C |

APPLICATION

Follow standard thick film procedure and screen Silver Epoxy Paste onto substrate using 165 or 200 mesh stainless steel screen. Mount parts to be bonded within a half hour and press lightly. Then oven cure at 150o C followed by at least 1 hour at 200oC.

Transene Co. Inc. 10 Electronics Ave, Danvers, MA 01923 Tel: 978-777-7860 Fax: 739-5640 www.transene.com

MICROCIRCUIT SILVERS

for Conductive Bonding in Microelectronics

One-part thermosetting silver epoxy systems for conductive bonding in microelectronic assembly operations.

MICROCIRCUIT SILVER - TYPE  K

Low temperature, fast cure- automatic dispensing

MICROCIRCUIT SILVER - TYPE L

Low temperature, fast cure - screen print

MICROCIRCUIT SILVER - TYPE N

High bond strength - 100% solids

MICROCIRCUIT SILVER - TYPE O

High electrical conductivity - 100% solids

TRANSENE COMPANY, INC. 10 Electronics Ave, Danvers Ma. 978-777-7860 fax 739-5640 www.transene.com

##### MICROCIRCUIT SILVERS

Microcircuit Silvers are one-part, thermosetting silver-epoxy compositions designed specifically for conductive bonding in microelectronic assembly operations. Recommended applications include the conductive bonding of integrated circuit chips, capacitors, and other active and passive components.  Microcircuit Silvers meet Hi-Rel requirements for low outgassing, bond strength, and electrical conductivity.

Microcircuit Silvers withstand temperatures up to 350oC, allowing ultrasonic and thermal compression bonding of interconnecting wires. Microcircuit Silvers Types K and L will fully cure in 15 seconds at 300oC; thus these silver compositions possess the unique ability to cure during thermal compression bonding operations.

Several modifications of Microcircuit Silvers are offered. Types K and L exhibit low temperature and fast cures. Types N and O are 100% solid systems and providing high electrical conductivity. Microcircuit Silvers Type K,L,N, and O are designed for screen printing or automatic dispensing applications.

Properties of Microcircuit Silvers

|  | Type K | Type L | Type N | Type O |
| --- | --- | --- | --- | --- |
| Uncured |  |  |  |  |
| Percent Silver | 75 | 73 | 70 | 77 |
| Solids (%) | 98 | 98 | 100 | 100 |
| Viscosity cps | 60,000 | 80,000 | 100,000 | 125,000 |
| Shelf Life-70oF | > 6 months | > 6 months | 6 months | 6 months |
| Application | Automatic dispense | Screen print/dispense | Screen print/dispense | Screen print |
| Cured |  |  |  |  |
| Serv. Temp Range | -50oC to + 175oC (325oC intermittent) | same | -60oC to + 200oC (325o intermittent) | same |
| Electrical Resistivity | 5 x 10-4 | 5 x 10-4 | 2 x 10-3 | 6 x 10-4 |
| Linear Coef. Therm Exp. (cm/cmoC) | 5 x 10-5 | same | same | same |
| Thermal Conductivity (BTU hr/ft2/oF/in.) | 21 | 20 | 20 | 22 |
| Outgassing |  |  |  |  |
| 1000 hrs @ 100oC | 0.05% | .05% | .09% | .08% |
| 1000 hrs @ 125oC | 0.2% | .2% | .7% | .6% |
| Bond Shear Strength (psi) after cure | 1500 | >1500 | 3500 | 1500 |
| aged 200 hrs @ 175oC | >1000 | >1000 | 2750 | 1000 |
| Cure Schedule |  |  |  |  |
| Select Temp.) |  |  |  |  |
| 115oC | - 1 1/2 hrs | 1 1/2 hrs | ---- | ---- |
| 125oC | 1 hr. | 1 hr. | ---- | ---- |
| 135oC | 30 min | 30 min | 5 hrs | 5 hrs. |
| 150oC | 15 min | 15 min | 1 1/2 hrs. | 1 1/2 hrs. |
| 175oC | 5 min | 5 min | 30 min | 30 min |
| 300oC | 15 sec. | 15 sec. | ---- | ---- |

Transene Co. Inc.  10 Electronics Ave, Danvers, MA 01923 Tel: 978-777-7860 Fax: 739-5640 www.transene.com

###### SILVER BOND

Low Temperature Thermosetting Silver

Epoxy silver compositions for conductive bonding in microelectronic assembly applications

SILVER-BOND - TYPE 40

Standard low-temperature cure, high electrical conductivity

SILVER-BOND - Type 50

Fast low-temperature cure, high electrical conductivity

SILVER-BOND - TYPE 60

Long pot life, fast cure

FEATURES

- Low temperature curing systems

- High bond strength

- Electrical resistivity < 10-4ohm-cm

- Low outgassing

- Long pot life

- Adhesive bonding to glass, metal, ceramic, plastics, graphite, quartz

Transene Co. Inc.  10 Electronics Ave, Danvers, MA 01923 Tel: 978-777-7860 Fax: 739-5640 www.transene.com

SILVER-BOND Conductive Adhesive

Description

Silver-Bond is a two component, epoxy based conductive adhesive for quality electrical and mechanical contacts. It provides high bond strength and excellent conductivity as well as low-temperature cure and long pot life. The product is designed for conductive bonding applications in microelectronics in place of lead tin solder or other alloys to avoid flux contamination or exposure to excessive temperature, and for process simplification. Silver-Bond Type 40 is especially recommended for bonding applications where it is desirable to keep process temperatures in the 100oC range. Silver-Bond Type 50 is modified for faster curing applications. Silver-Bond Type 60 provides extended pot-life with fast cure at slightly elevated temperatures.

PROPERTIES OF SILVER-BOND

|  | Type 40 | Type 50 | Type 60 |
| --- | --- | --- | --- |
| Composition | Silver Filled Epoxy | same | same |
| Consistency | Soft Thixotropic paste | same | same |
| Viscosity | 90,000 cps  10% | same | same |
| Elect. Resitivity | 1 x 10-4 ohm-cm max. | same | same |
| Lap Shear strength | 1500 psi nominal | same | same |
| Temperature stability range | -65oC to + 200oC | -65oC to + 175oC | -65oC to + 175oC |
| Outgassing (postcure) | <.01%/100 hr. @ 125oC | same | same |
| Thermal conductivity | 80 BTU/in/ft2hr/oC | same | same |
| Pot life | 6 hrs at 25oC | 2 hrs at 25oC | 48 hrs at 25oC |
| Shelf life | one year @ 25oC | same | same |
| Cure (at 100oC) | 2 hrs | 10 minutes | 10 minutes |
| Thinner | Butyl Cellosolve Acetate | same | same |
| Mixing Ratio (A:B) (by wt.) | 100/3.6 | 100/2.5 | 100/2.5 |
| Part A | Part B | Part B | Part B |
| 1 gm | 0.036 gm (1 drop) | 0.024 gm (1 drop) | Same as type 50 |
| 5 gms | 0.180 gm (6 drops) | 0.124 gm (4 drops) |  |
| 1 oz. (28.35 gms) | 1.023 gms (34 drops) | 0.76 gm (24 drops) |  |
| Cure Schedule (Time -Temp.Relationship) 50oC 75oC 100oC 125oC 150oC | ---- 2 1/2 hrs. 2 hrs. 1 1/2 hrs. 1 hr. | 30 minutes 15 minutes 10 minutes 5 minutes ---- | ---- ---- 10 minutes 5 minutes 2 minutes |

Transene Co. Inc. 10 Electronics Ave, Danvers, MA 01923 Tel: 978-777-7860 Fax: 739-5640 www.transene.com

NANOPOXY 60

Electrically Conductive Epoxy for Nanoscale Applications

DESCRIPTION

Nanopoxy 60 is a two component, epoxy-based conductive adhesive for nanoscale electrical contacts. Nanopoxy 60 provides excellent bond strengths, long pot life, low temperature cure, low resistivity, and minimal outgassing. A micron-scale conductive flake is employed to provide good conductivity for nanotubes and other nano materials. Nanopoxy 60 is ideal for SEM environments, offering long pot life and quick cure for ease of handling.

| PROPERTIES |  |
| --- | --- |
| Appearance | Silver filled epoxy paste |
| Viscosity | 80,000 - 100,000 cps |
| Electrical Resistivity | 1 x 10-3 ohm-cm |
| Outgassing (postcure) | <0.01%/100 hr @ 25oC |
| Thermal Conductivity | 80 BTU-in/ft2 hr/ oC |
| Pot Life | 48 hrs @ 25oC |
| Shelf Life | 1 year @ 25OC |
| Temp. Stability Range | -65oC to 175oC |
| Thinner | Butyl Cellosolve Acetate |

| MIXING RATIO (A:B) by wt. 100:2.5 |  |
| --- | --- |
| Part A | Part B |
| 1 gram | 1 drop |
| 5 grams | 4 drops |
| 1 oz (28.35 grams) | 24 drops |
| CURE SCHEDULE |  |
| Temperature | Time |
| 100oC | 10 min. |
| 125oC | 5 min. |
| 150oC | 2 min. |

APPLICATIONS

Nanopoxy 60 is designed to facilitate electrical conductivity measurements of nanotubes. With a mean particle size below 3 microns, Nanopoxy 60 is effective at providing electrical contacts even for nanotubes with diameters under 30 nanometers. The epoxy resin system provides excellent adhesion to most nano materials such as carbon or tungsten disulfide nanotubes, nanowires, and other nano device components.

Transene Company, Inc. 10 Electronics Ave. Danvers MA 01923 978-777-7860 fax: 978-739-5640 www.transene.com

GOLD - EPOXY PASTE

THERMOSETTING GOLD FOR OHMIC BONDING

Produces quality electrical and mechanical contacts for semiconductor and hybrid circuits applications.

GOLD-EPOXY PASTE, TYPE GE-10

One-part system, economical

GOLD-EPOXY PASTE, TYPE GE-20

Two-part system, low temperature cure

GOLD EPOXY PASTE, TYPE GE-30

Two-part system, fast cure

GOLD-EPOXY PASTE, TYPE GE-40

Two-part system, fast cure, long pot life

Transene Co. Inc.  10 Electronics Ave, Danvers, MA 01923 Tel: 978-777-7860 Fax: 739-5640 www.transene.com

GOLD EPOXY PASTE

DESCRIPTION

Gold-Epoxy Pastes are gold-filled conductive bonding preparations exhibiting high electrical conductivity and bond strength.

The Gold Pastes are easily applied by manual technique, machine dispensing or screen printing and cured with relatively low applied heat in bonding operations. Gold-Epoxy Pastes are used to advantage in place of tin-lead solders to avoid flux contamination or exposure of components to excessive heat. The gold products are used in preference to silver-epoxy or other silver preparations to avoid silver migration problems.

Gold-Epoxy Pastes bond well to alumina ceramic substrates, phenolic circuit boards and transistor headers. They are useful in a variety of applications in solid state and hybrid circuits including:

- Attachment of discrete semiconductor devices and integrated circuits. Ohmic contacts are produced with diodes and transistors, in all package configurations, if the semiconductor surface is first metallized or the surface is highly “doped” and lapped.

- Bonding of other active devices, heat sinks and capacitor chips.

3. Top electrodes for crossovers and interconnections for parallel and multipurpose circuits.

Gold-Epoxy Paste, Type GE-10 is more economical to use since it is a one-part system with waste eliminated in actual use. Types GE-20 and GE-30 are two-part systems and cure more rapidly and at lower temperatures. Type GE-30 is especially recommended for repair of microcircuitry. Type GE-40 is formulated for long pot life and fast cure. It is recommended for screen print applications. All of the Gold-Epoxy Pastes are designed for low outgassing and for continuous use up to 175oC.

PROPERTIES OF GOLD-EPOXY PASTES

|  | Gold Epoxy GE-10 | Gold Epoxy GE-20 | Gold Epoxy GE-30 | Gold Epoxy GE-40 |
| --- | --- | --- | --- | --- |
| Composition | 88% Gold | 88% Gold | 88% Gold | 88% Gold |
| System | One-part epoxy | Two-part epoxy | Two-part epoxy | Two-part epoxy |
| Viscosity(cps) | 175,000 | 175,000 | 175,000 | 175,000 |
| Rheology | Thixotropic paste | Thixotropic paste | Thixotropic paste | Thixotropic paste |
| Pot Life (25oC) | 6 months | 6 hours | 2 hours | 2 days |
| Shelf Life | 6 months | 1 year | 1 year | 1year |
| Application | Screen printing or dispensing | Screen printing or dispensing | Dispensing | Screen printing or dispensing |
| Thinner | Butyl carbitol acetate or butyl cellosolve acetate | Butyl carbitol acetate or butyl cellosolve acetate | Butyl cellosolve acetate | Butyl carbitol acetate or butyl cellosolve acetate |
| Cure | 15 hours. @150oC, or 1 hr. @ 150oC plus 2 hrs @ 200oC | 4 hrs @ 50oC, or 2 1/2 hrs @ 75oC or 2 hrs @ 100oC | 1/2 hr @ 50oC or 15 min @ 75oC or 5 min @ 125oC. | 10 min @ 100oC or 5 min @ 125oC or 2 min @ 150oC |
| Elec. Resist,(Ohm-cm) | 4 x 10-4 | 7 x 10-4 | 7 x 10-4 | 6 x 10-4 |
| Bond Shear Str. (psi) | 1000 | 1000 | 1000 | 1000 |
| Outgassing (postcure) 1000 hrs @ 125oC | 0.70% | 0.30% | 0.35% | 0.30% |
| Serv. Temp Range | -65o to + 200oC | -65o to + 175oC | -65o to + 175oC | -65o to + 175oC |
| Mixing Ratio (a/b) | ------------------------ | (100/1.8) | (100/1.3) | (100/2.7) |
|  |  | A B 1.25 gm 1 drop 10 gm 7 drops 1 oz. 22 drops | A B 2 gm 1 drop 10gm 5 drops 1 oz. 16 drops | A B 2 gm 2 drops 10gm 9 drops 1 oz. 24 drops |

TRANSENE COMPANY, INC. 10 Electronics Ave, Danvers Ma. 978-777-7860 fax 739-5640 www.transene.com

GOLD EPOXY CONTINUED

APPLICATION:

Gold-Epoxy Pastes are applied by screening using a 200 mesh stainless steel screen, or by other methods of application such as dotting with a needle or by use of automatic dispensing equipment.  Parts to be bonded are mounted and pressed lightly then over-cured under the appropriate conditions of time and temperature.

##### Transene Co. Inc.  10 Electronics Ave, Danvers, MA 01923 Tel: 978-777-7860 Fax: 978-739-5640 www.transene

##### POLYIMIDE DIE ATTACH ADHESIVES

Low Mobile Ion, Silver-filled Adhesive for IC Chip Bonding

DESCRIPTION

One-component, silver-filled TRANSENE POLYIMIDE DIE ATTACH ADHESIVES are heat-cured to provide unparalleled high temperature performance (to 500oC) and excellent electrical conductivity ( < 1 x 10-4 ohm-cm). These ultra-pure polyimide-based adhesives exhibit extremely low levels of extractable ionic impurities (Cl, Na, K) less than 10 ppm.

TRANSENE POLYIMIDE DIE ATTACH ADHESIVES maintain high electrical conductivity, high thermal conductivity and outstanding adhesive strengths to 500oC (375oC) for 200 hrs. Under severe moisture conditions, the polyimide based adhesives exhibit less corrosivity than epoxies. These polyimide die attach adhesives are fluoride and phosphate free, allowing compatibility with aluminum metallization.

|  | METHOD | % SILVER | VISCOSITY |
| --- | --- | --- | --- |
| TRANSENE PDA S-500 | SCREEN/STAMP | 72 | 90,000 10% |
| TRANSENE PDA D-500 | DOT DISPENSER | 68 | 60,000 10% |

PROPERTIES

| Consistency | Soft smooth paste |
| --- | --- |
| Filler | Pure silver flake |
| Resin type | Polyimide |
| Thermal Conductivity | 90 BTU/ft2/hr/oF/in |
| Volume resistivity: -35oC to + 400oC 300 hrs. @ 370oC | 1 x 10-4 ohm-cm 1 x 10-4 ohm-cm |
| Bond Shear Strength |  2,000 psi @ 25-150oC,  1,500 psi @ 300oC |
| Ionic Impurities | Cl  10 ppm, Na  5 ppm, K  5 ppm |
| Operating Temperature | Cont: -45 to + 375oC, Intermittent: 500oC |
| Non-Corrosive | No fluorides or phosphates |
| Cure | 150oC for 15 min. PLUS 270oC for 30 minutes |
| Shelf Life | 25oC -2 months, 0oC - 6 months |

APPLICATION:

TRANSENE POLYIMIDE DIE ATTACH ADHESIVES applications include: IC chip bonding on plastic and ceramic substrates, DIP memory chips and other electronic and aerospace assemblies requiring high temperature capability. Adhesive strengths ( @ 300oC) of greater than 1500 PSI are typically achieved. Subsequent processing temperatures to 500oC (ceramic package sealing and brazing operations) will cause no adverse effects to die attach performance.  Apply PDA adhesive by screen/stamp or “dot” technique. Place die, chip or component in place and commence two-step cure. The initial cure temperature will dissipate solvent and the higher temperature will imidize the resin system.

#### TRANSENE CO. INC.  10 Electronics Ave, Danvers, MA 01923 Tel: 978-777-7860 Fax: 739-5640 www.transene.com

## SURFACE MOUNT ADHESIVES

Low cost, high density packaging of integrated circuits, lead-less chip carriers, and chip component attachment for ceramic substrates and PC Boards

TRANSENE SMA EPOXY ADHESIVES are formulated specifically for precision mounting of flat pack semiconductor devices, chip capacitors and resistors in the production of complex hybrid circuits. Preliminary physical attachment (staking) prior to wave soldering leaded devices or the direct mounting of discrete components and microwave devices (dual-in-line pack) is feasible for both electrically conductive and non-conductive attachment.

TRANSENE SMA EPOXY ADHESIVES include 1 and 2 part systems, supplied in customized packages to interface application techniques for auto-dispensing or screen printing. The various formulations offer non-corrosive systems with good handling characteristics-thixotropy resistant to trailing/stringing and adequate body to fill gaps and crevices. Quick cure, good adhesion, and ability to withstand mechanical and thermal stress, wave soldering temperatures and clean-up solvents provide for wide application.

COLOR CUSTOMIZING AVAILABLE

# PROPERTIES OF SURFACE MOUNT ADHESIVES

|  | SMA-100 | SMA-200 | SMA-300 | SMA-400 | SMA-500 | SMA-600 | SMA-700 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Feature | High Thermal Conductiviy | Low Moisture absorbtion | Staking Compound-Quick Cure | Hi Therm Conductivity Low Temp Cure | Standard | Low Temp Cure | Long Pot Life |
| Application | Auto-Dispense | Auto-Dispense | Auto -Dispense | Auto-Dispense | Auto Dispense Screen print | Auto Dispense | Auto Dispense Screen Print |
| Composition | 1 part / Filled | 1 part / Filled | 2 part / Unfilled | 2 part / Filled | 1 part | 2 part | 2 part |
| Color | Red | Green | Amber | Black | Silver paste | Silver paste | Silver paste |
| Viscosity | 100,000 cps | 90,000 cps | 20,000 cps | 70,000 cps | 80,000 cps | 90,000 cps | 90,000 cps |
| Shelf-Life @ 25oC | 6 months | 6 months | 6 months | 6 months | 6 months | 12 months | 12 months |
| Thermal Cond. BTU/hr/ft2/in/oF | 12 | 4 | -- | 10 | 75 | 80 | 80 |
| Coef. of Thermal exp(in/in/oCx10-6) | 23 | 30 | -- | 20 | 50 | 60 | 60 |
| Lap Shear | 1500 psi | 2000 psi | 2000 psi | 2000 psi | 1500 psi | 1500 psi | 1500 psi |
| Moisture Absorption | 0.14% | 0.05% | -- | 0.17% | -- | -- | -- |
| (7 day imm.@ 25oC) |  |  |  |  |  |  |  |
| Vol resistivity (ohm/cm) | 1 x 10-16 | 1 x 10-15 | 1 x 10-15 | 1 x 10-15 | 1 x 10-4 | 1 x 10-4 | 1 x 10-4 |
| Dielectric strength (v/mil) | 500 | 450 | 400 | 450 | --- | --- | --- |
| Mix Ratio | --- | --- | 1:1 | 100:7 | --- | 100:3.6 | 100:2.5 |
| CURE | 115oC-30min | 115oC - 30min | 25oC-1hr | 50oC-20 min | 125oC-1hr | 50oC-30 min | 100oC-10min |
|  | 135oC-1 min | 135oC15min | ---- | 75oC-10min | 150oC-5min | 75oC-15min | 125oC-5min |
| Pot Life | --- | --- | 10 min | 3 hrs | --- | 2 hrs | 40 hrs |

CONDUCTIVE VIA FILL CVF-6030

DESCRIPTION

Conductive Via Fill CVF-6030 is a two-part filled epoxy system designed to provide electrical and thermal conductivity in PWB and PBGA applications.  Applied via stencil, CVF-6030 is an effective, economical fill for vias.  When planarized, CVF-6030 is receptive to plating and soldering.  Because the via fill exhibits no shrinkage, electrical and thermal conductivity are retained during curing.  Vias up to 0.75 mm diameter may be filled with excellent results.  The long pot life of CVF-6030 enhances clean-up while its fast cure reduces processing time.  Because CVF-6030 is a two-part system, material may be left at room temperature for extended periods, further enhancing processing.

PROPERTIES

| System | Two-Part |
| --- | --- |
| Composition | Silver filled epoxy |
| Viscosity | 110,000-140,000 cps |
| Thinner | CVF-6030 Thinner |
| Electrical Resistivity, nominal | 3 x 10-4 ohm-cm |
| Thermal Conductivity | > 100 BTU/ft2/hr./oF./in. |
| Outgassing | < 0.01%/100 hours @ 125 oC |
| Stencil Type | 3-4 stainless steel |
| Aspect Ratio (depth:diameter) | 6:1 |
| Clean-up Solvent | Iso-propyl alcohol; acetone |
| Temperature Stability Range | -65 oC to + 175 oC |
| Storage | Room Temperature |
| Shelf Life | 1 year @ 25 oC |
| Pot Life Mixing Ratio | 48 hours @ 25 oC 4 drops (0.124 grams) Part B per 10 grams Part A |
| Cure Schedule | 100 oC for 30 minutes |
|  | Or 125 oC for 20 minutes Or 150 oC for 15 minutes |

INSTRUCTIONS

CVF-6030 may be applied via stencil to drilled, plated through holes and is then cured as instructed.  The stencil heads of the cured via fill may be removed by planarazation to yield a smooth, uniform surface.  It is then possible to electroplate prior to printing and etching or proceed directly to the print and etch process.

Special Thinner included

#### Transene Company Inc. 10 Electronics Avenue, Danvers MA 01923 Tel: 978-777-7860 Fax: 978-739-5640 www.transene.com

Transene Technical Literature

| Catalog #1 |  | Semiconductor Etchants Material for Electronics |
| --- | --- | --- |
| Catalog #2 | Thin Film Catalog Thin Film Etchant for Microelectronics Circuits |  |
| Catalog #3 | Semiconductor Materials Cleaning-Polishing, Diffusants,Vacuum Pump Fluid, Thermal Grease, Junction Coatings, Photoconductors |  |
| Catalog #4 | Conformal Coatings |  |
| Catalog #5 | Electroless & Electroplating Products |  |
| Catalog # 6 | PC Board Circuit Materials |  |
| Catalog #7 | Encapsulants For Electronic Packaging |  |
| Catalog #8 | Epoxy Temperature Metallizing |  |

TRANSENE CO. INC. 10 Electronics Ave Danvers, MA 01923

978-777-7860 Fax: 978-739-5640 www.transene.com